# Pavement Profiles

C.G. Hoehne

07 June, 2019

Bare Ground Profiles

| profile | layer | thickness | k | rho | c | albedo | emissivity |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Bare Dry Soil #1 | surface | 0.75 | 1.8 | 2000 | 1900 | 0.40 | 0.900 |
| Bare Dry Soil #1 | subgrade | 0.75 | 1.8 | 2000 | 1900 | NA | NA |
| Bare Dry Soil #2 | surface | 0.75 | 1.4 | 1750 | 1500 | 0.45 | 0.935 |
| Bare Dry Soil #2 | subgrade | 0.75 | 1.4 | 1750 | 1500 | NA | NA |
| Bare Dry Soil #3 | surface | 0.75 | 1.0 | 1500 | 1100 | 0.50 | 0.970 |
| Bare Dry Soil #3 | subgrade | 0.75 | 1.0 | 1500 | 1100 | NA | NA |

Asphalt Surfaced Pavement Profiles

| profile | layer | thickness | k | rho | c | albedo | emissivity |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Asphalt 80mm | surface | 0.08 | 1.70 | 2350 | 950 | 0.15 | 0.9 |
| Asphalt 80mm | base | 0.10 | 2.25 | 2350 | 875 | NA | NA |
| Asphalt 80mm | subgrade | 1.32 | 1.40 | 1850 | 1500 | NA | NA |
| Asphalt 140mm | surface | 0.14 | 1.70 | 2350 | 950 | 0.15 | 0.9 |
| Asphalt 140mm | base | 0.20 | 2.25 | 2350 | 875 | NA | NA |
| Asphalt 140mm | subgrade | 1.16 | 1.40 | 1850 | 1500 | NA | NA |
| Asphalt 200mm | surface | 0.20 | 1.70 | 2350 | 950 | 0.15 | 0.9 |
| Asphalt 200mm | base | 0.30 | 2.25 | 2350 | 875 | NA | NA |
| Asphalt 200mm | subgrade | 1.00 | 1.40 | 1850 | 1500 | NA | NA |
| Asphalt Overlay on PCC 100+100mm | surface | 0.10 | 1.70 | 2350 | 950 | 0.15 | 0.9 |
| Asphalt Overlay on PCC 100+100mm | PCC | 0.10 | 1.70 | 2250 | 900 | NA | NA |
| Asphalt Overlay on PCC 100+100mm | base | 0.10 | 2.25 | 2400 | 800 | NA | NA |
| Asphalt Overlay on PCC 100+100mm | subgrade | 1.06 | 1.40 | 1850 | 1500 | NA | NA |
| Asphalt Overlay on PCC 125+150mm | surface | 0.13 | 1.70 | 2350 | 950 | 0.15 | 0.9 |
| Asphalt Overlay on PCC 125+150mm | PCC | 0.15 | 1.70 | 2250 | 900 | NA | NA |
| Asphalt Overlay on PCC 125+150mm | base | 0.20 | 2.25 | 2400 | 800 | NA | NA |
| Asphalt Overlay on PCC 125+150mm | subgrade | 1.02 | 1.40 | 1850 | 1500 | NA | NA |
| Asphalt Overlay on PCC 150+200mm | surface | 0.15 | 1.70 | 2350 | 950 | 0.15 | 0.9 |
| Asphalt Overlay on PCC 150+200mm | PCC | 0.20 | 1.70 | 2250 | 900 | NA | NA |
| Asphalt Overlay on PCC 150+200mm | base | 0.30 | 2.25 | 2400 | 800 | NA | NA |
| Asphalt Overlay on PCC 150+200mm | subgrade | 0.85 | 1.40 | 1850 | 1500 | NA | NA |

Concrete Surfaced Pavement Profiles

| profile | layer | thickness | k | rho | c | albedo | emissivity |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Portland Cement Concrete 100mm | surface | 0.20 | 1.70 | 2250 | 945 | 0.2 | 0.90 |
| Portland Cement Concrete 100mm | base | 0.20 | 2.25 | 2400 | 800 | NA | NA |
| Portland Cement Concrete 100mm | subgrade | 1.10 | 1.40 | 1850 | 1500 | NA | NA |
| Portland Cement Concrete 200mm | surface | 0.20 | 1.70 | 2250 | 945 | 0.3 | 0.93 |
| Portland Cement Concrete 200mm | base | 0.20 | 2.25 | 2400 | 800 | NA | NA |
| Portland Cement Concrete 200mm | subgrade | 1.10 | 1.40 | 1850 | 1500 | NA | NA |
| Portland Cement Concrete 300mm | surface | 0.20 | 1.70 | 2250 | 945 | 0.4 | 0.96 |
| Portland Cement Concrete 300mm | base | 0.20 | 2.25 | 2400 | 800 | NA | NA |
| Portland Cement Concrete 300mm | subgrade | 1.10 | 1.40 | 1850 | 1500 | NA | NA |
| Whitetopped Asphalt 80+80mm | surface | 0.08 | 1.70 | 2250 | 945 | 0.3 | 0.93 |
| Whitetopped Asphalt 80+80mm | asphalt | 0.08 | 1.70 | 2350 | 950 | NA | NA |
| Whitetopped Asphalt 80+80mm | base | 0.10 | 2.25 | 2400 | 800 | NA | NA |
| Whitetopped Asphalt 80+80mm | subgrade | 1.24 | 1.40 | 1850 | 1500 | NA | NA |
| Whitetopped Asphalt 100+140mm | surface | 0.10 | 1.70 | 2250 | 945 | 0.3 | 0.93 |
| Whitetopped Asphalt 100+140mm | asphalt | 0.14 | 1.70 | 2350 | 950 | NA | NA |
| Whitetopped Asphalt 100+140mm | base | 0.20 | 2.25 | 2400 | 800 | NA | NA |
| Whitetopped Asphalt 100+140mm | subgrade | 1.06 | 1.40 | 1850 | 1500 | NA | NA |
| Whitetopped Asphalt 150+200mm | surface | 0.15 | 1.70 | 2250 | 945 | 0.3 | 0.93 |
| Whitetopped Asphalt 150+200mm | asphalt | 0.20 | 1.70 | 2350 | 950 | NA | NA |
| Whitetopped Asphalt 150+200mm | base | 0.30 | 2.25 | 2400 | 800 | NA | NA |
| Whitetopped Asphalt 150+200mm | subgrade | 0.85 | 1.40 | 1850 | 1500 | NA | NA |