Table 1. Summary of material parameters ranges used for asphalt, concrete, and subgrade from literature. Note that layer thicknesses vary by functional class and layer type (e.g. surface, overlay, base, subbase, etc.). Note that “Ground” refers to bare, native, and uncompacted material in the Phoenix region (i.e. desert soil or sand) that would represent undeveloped land. “Subgrade” refers to compacted materials underneath the pavement.

| Parameter | Units | Asphalt | Concrete | Subbase | Ground or Subgrade* |
| --- | --- | --- | --- | --- | --- |
| Albedo, α | dimension-less | 0.05 – 0.15 a 0.08 – 0.09 b 0.17 c | 0.18 – 0.29 b 0.20 – 0.40 a 0.31 – 0.43 c | NA | 0.30 d 0.40 – 0.50 e |
| Emissivity, ε | dimension-less | 0.85 c, f 0.90 g 0.90 – 0.95 h | 0.90 i 0.92 – 0.96 j | NA | 0.90 – 0.97 d |
| Thermal conductivity, k | Wm∙K | 1.2 c 1.4 – 1.8 k 1.5 g 1.6 l 1.9 – 2.2 m | 1.2 n 1.2 – 1.4 j 1.5 i 2.2 l | 1.5 g 3.0 l | 1.0 c 1.2 l 1.8 g |
| Density, ρ | kgm3 | 2200 c 2300 m 2300 – 2500 k 2400 – 2600 g 1800 – 2500 n | 1810 – 2100 j 2300 n 2400 i | 2400 g | 1500 c 2200 g |
| Specific heat capacity, c | Jkg∙K | 810 – 960 j 850 – 860 g 900 n 920 j 1200 – 1900 k | 840 – 1050 j 1000 i | 800 g | 1100 g 1900 c |
| Layer thickness | mm | 40 – 200 n, o, p | 100 – 300 o, q | 100 – 300 n, o, p | NA |

a (Qin, 2015)

b (Li et al., 2013)

c (Gui et al., 2007)

d (Monteith & Unsworth, 2013)

e (Dobos, 2011)

f (Hermansson, 2004)

g (Minhoto et al., 2006)

h (Tan & Fwa, 1992)

i (Bentz & Turpin, 2007)

j (Hu et al., 2017)

k (Luca & Mrawira, 2005)

l (Wang & Roesler, 2012)

m (Im et al., 2015)

n (Hall et al., 2012)

o (ADOT, 2017)

p (FAA, 2016)

q (USACE, 2018)

# References

ADOT, (Arizona Department of Transportation). (2017). Pavement Design Manual. Retrieved from https://apps.azdot.gov/files/materials-manuals/Preliminary-Engineering-Design/PavementDesignManual.pdf

Bentz, D. P., & Turpin, R. (2007). Potential applications of phase change materials in concrete technology. Cement and Concrete Composites, 29(7), 527–532. https://doi.org/10.1016/j.cemconcomp.2007.04.007

Dobos, E. (2011). Encyclopedia of Soil Science, Second Edition. https://doi.org/10.1081/E-ESS

FAA, (Federal Aviation Administration). (2016). Airport Pavement Design and Evaluation. https://doi.org/150/5320-6F

Gui, J., Phelan, P. E., Kaloush, K. E., & Golden, J. S. (2007). Impact of Pavement Thermophysical Properties on Surface Temperatures. Journal of Materials in Civil Engineering, 19(8), 683–690.

Hall, M. R., Dehdezi, P. K., Dawson, A. R., Grenfell, J., & Isola, R. (2012). Influence of the Thermophysical Properties of Pavement Materials on the Evolution of Temperature Depth Profiles in Different Climatic Regions. Journal of Materials in Civil Engineering, 24(1), 32–47. https://doi.org/10.1061/(ASCE)MT.1943-5533.0000357

Hermansson, Å. (2004). Mathematical model for paved surface summer and winter temperature: comparison of calculated and measured temperatures. Cold Regions Science and Technology, 40(1–2), 1–17. https://doi.org/10.1016/j.coldregions.2004.03.001

Hu, L., Li, Y., Zou, X., Du, S., Liu, Z., & Huang, H. (2017). Temperature Characteristics of Porous Portland Cement Concrete during the Hot Summer Session. Advances in Materials Science and Engineering, 2017. https://doi.org/10.1155/2017/2058034

Im, J. S., Dessouky, S., Bai, B. C., Vo, H. V., & Park, D.-W. (2015). Thermal Properties of Asphalt Mixtures Modified with Conductive Fillers. Journal of Nanomaterials, 2015, 1–6. https://doi.org/10.1155/2015/926809

Li, H., Harvey, J., & Kendall, A. (2013). Field measurement of albedo for different land cover materials and effects on thermal performance. Building and Environment, 59, 536–546. https://doi.org/10.1016/J.BUILDENV.2012.10.014

Luca, J., & Mrawira, D. (2005). New Measurement of Thermal Properties of Superpave Asphalt Concrete. Journal of Materials in Civil Engineering, 17(1), 72–79. https://doi.org/10.1061/(ASCE)0899-1561(2005)17:1(72)

Minhoto, M. J. C., Pais, J. C., & Pereira, P. a. a. (2006). Asphalt Pavement Temperature Prediction. Asphalt Rubber 2006: Proceedings, 193–207. https://doi.org/10.1061/9780784413005.029

Monteith, J. L., & Unsworth, M. H. (2013). Principles of Environmental Physics: plants, animals, and the atmosphere (4th ed.). Academic Press.

Qin, Y. (2015). Urban canyon albedo and its implication on the use of reflective cool pavements. Energy and Buildings, 96, 86–94. https://doi.org/10.1016/j.enbuild.2015.03.005

Tan, S. A., & Fwa, T. F. (1992). Influence of pavement materials on the thermal environment of outdoor spaces. Building and Environment, 27(3), 289–295. https://doi.org/10.1016/0360-1323(92)90030-S

USACE, (United States Army Corps of Engineers). (2018). Unified Facilities Criteria. https://doi.org/UFC 3-201-01

Wang, D., & Roesler, J. R. (2012). One-Dimensional Rigid Pavement Temperature Prediction Using Laplace Transformation. Journal of Transportation Engineering, 138(9), 1171–1177. https://doi.org/10.1061/(ASCE)TE.1943-5436.0000413